Copperhead® Tracerwire Specification for

#16 Solid CCS SuperFlex - Break Load 113 lbs.

Part #s: 1630*-SF-500  /  1630*-SF-1000  /  1630*-SF-2500

Part # description: 16 (AWG), 30 (jacket mil), *(indicates jacket color: B=Blue, Y=Yellow, R=Red, K=Black, N=Orange, G=Green, P=Purple) – SF (SuperFlex) – 500, 1000 or 2500 (wire length in ft.)

Print Line:  Physical, permanent markings: surface legend print on insulating jacket to repeat at minimum interval of every two linear feet.  Ink colors will include: Black Ink for the following jacket colors: Yellow, Blue, Red, Orange, Purple and Green.  White Ink for Black jacket.

COPPERHEAD  * 16 AWG-SOLID SUPERFLEX SF-CCS TRACER WIRE * 30 MIL HDPE * 30 VOLT * DIRECT BURIAL ONLY

Spool Label:  Wound wire on a compact spool made of metal, plastic, or wood.

#### COPPERHEAD INDUSTRIES, LLC

#### 1630*-SF-500 (Production Trace Code)

#### 16 AWG-Solid CCS Tracer Wire

#### 30 Mil HDPE * 30 Volt

#### Direct Burial Only

#### www.copperheadwire.com

Product Description:

Tracer wire shall be a #16 AWG (0.0508” diameter) fully annealed, low carbon 1010 grade steel, solid copper-clad steel (CCS) conductor, insulated with a 30 mil, high-density, high molecular weight polyethylene (HDPE) insulation, and rated for direct burial use at 30 volts. CCS conductor must be at 21% conductivity for locating purposes. Break load of 113 lbs. HDPE insulation shall be RoHS compliant and utilize virgin grade material. Insulation color shall meet the APWA color code standard for identification of buried utilities. Tracer wire shall be Copperhead® SuperFlex CCS, HDPE 30 mil insulation or district pre-approved equal and made in the USA.

Copperhead Industries LLC, PO Box 1081 Monticello, MN 55362 ∙ Ph 877-726-5644 ∙ Fax 763-271-3694 www.copperheadwire.com

Recommended Engineering Specifications:

Conductor Specifications for SuperFlex Tracer Wire

#16 Solid CCS SuperFlex – Break Load 113 lbs.

Specification:  This specification describes the properties of the conductor to be used in the fabrication

of high strength tracer wire.

- Material Description: Copperhead( Copper-clad steel wire as manufactured by Copperweld® is composed of a steel core with a uniform and continuous copper cladding thoroughly bonded to the steel throughout.  Wire must conform to ASTM B910 / B910M

  - Cladding:  The steel and copper interface must have a metallurgical bond achieved through a high heat and pressure bonding process.  Established process for porosity-free material.

  - Steel: High Strength with 0.10 carbon or greater. Verified to meet required mechanical properties.

  - Copper: UNS-C10200; OF Copper according to ASTM B-170 (latest revision).  High

conductivity, oxygen free copper to achieve optimal signal performance.

- Surface Condition:  Wire surface shall be free of any defects, including flakes, grooves, pits, and

voids.  Wire surface shall be smooth, bright and shiny, and free of excessive copper dust and

residual drawing lubricants.

3.    Physical, Mechanical, and Electrical Properties

The wire shall conform to the properties listed in Table 1.

### TABLE 1: Physical, Mechanical, and Electrical Properties

| #16 CCS Low Carbon 1010 Steel Grade 21% Conductivity | CCS Conductor |
| --- | --- |
| Conductor Size | 16 AWG |
| Conductor Type | Copper Clad Steel (CCS) |
| Temper | Dead Soft Annealed (DSA) |
| Average Break Load | 113 lbs. |
| Minimum Tensile Strength | 48,000 psi |
| Minimum Elongation | 10.0% |
| Nominal Copper Thickness (% of Diameter) | 3.0% |
| Nominal Copper Weight | 13% |
| Nominal DC Resistance (ohms/1000 ft.) | 19.137 |

*Diameter tolerances:  ± 1%

Copperhead Industries LLC, PO Box 1081 Monticello, MN 55362 ∙ Ph 877-726-5644 ∙ Fax 763-271-3694 www.copperheadwire.com

Insulating Jacket Specifications for SuperFlex Tracer Wire

#16 Solid CCS SuperFlex – Break Load 113 lbs.

Specification:  This specification describes the properties of the insulation material to be used in the

jacketing of high strength tracer wire.

1.  Material Description: insulating jacket is comprised of a co-polymer high molecular weight natural

high density polyethylene (HDPE) designed specifically for high-speed copper wire insulating.  It contains the required levels and types of primary antioxidant and metal deactivator additives to satisfy most Wire and Cable industry requirements.  HDPE material will be produced with an excellent balance of surface smoothness, processing ease, tensile and elongation properties, abrasion toughness, environmental stress crack, thermal stress crack resistance, and electrical consistency.

2.  Physical, Mechanical, and Electrical Properties

The wire shall conform to the properties listed in Table 1.

### TABLE 1: Physical, Mechanical, and Electrical Properties

| High Density Polyethylene Insulator | Value |
| --- | --- |
| Density (ASTM D 792) | 0.943 g/cc |
| Bulk Density (ASTM D 1895) | 0.58 g/cc |
| Melt Index (ASTM D 1238/E) | 0.70 dg/min |
| Tensile-Yield (ASTM D 638) | 4300 psi |
| Tensile-Ultimate (ASTM D 638) | 2900 psi |
| Tensile-Elongation (ASTM D 638) | 850% |
| Flexural Modulus (ASTM D 790/1) | 120,000 psi |
| Hardness (ASTM D 2240) | 63 Shore D |
| Environmental Stress-Crack (ASTM D 1693/B) | F20 > 48 h |
| Thermal Stress-Crack (ASTM D2951) | F0 > 1000 h |
| Brittleness Temperature (ASTM D 746) | < -95( F |
| Melting Point (DSC) (ASTM D 3417) | 262( F |
| Softening Point (Vicat) (ASTM D 1525) | 250( F |
| Oxidative Induction Time (ASTM D 3895) | > 50 min. @ 200( C |
| Dielectric Constant (ASTM D 1531) | 2.34 @ 1MHz |
| Dissipation Factor (ASTM D 1531) | 0.00007 @ 1 MHz |
| Volume Resistivity (ASTM D 257) | 5 x 1017 ohm-cm |
| Dielectric Strength (ASTM D 3755) | 1000 volts @ 20 mils |

Copperhead Industries LLC, PO Box 1081 Monticello, MN 55362 ∙ Ph 877-726-5644 ∙ Fax 763-271-3694 www.copperheadwire.com